| Definitions |
| --- |
| You may not have heard of some of the terms used in this lesson before. Here are some definitions that might be helpful. |
| Stress Stress is a relationship between the force applied to an object and the area over which it acts. | Tensile strength The tensile strength of a material is the maximum tensile stress it can withstand before it breaks. The units are the same as for stress, Newtons per square metre (N/m2). |
| Strain If we take a wire or rod and apply a pulling force to the ends, the object will be under tension and it will stretch slightly. Strain is a measure of how stretchy an object is. Strain = change in length or extension original length As strain is a ratio of two lengths, it has no units. | Modulus of elasticity This is sometimes known as the Young modulus and it is a measure of the stiffness of a material. The greater a material’s modulus of elasticity, the greater its stiffness or resistance to being stretched. It has the same units as stress and tensile strength, Newtons per square metre (N/m2). |